| 1252-10, Jungwang-Dong, Shihung City Kyonggy-Do, Korea, 429-450 Tel:(031) 499-1921-4, Fax:(031) 498-1601 | 難 燃 劑 (Flame Retardant Chemical) | File No. | WJ-007 |
| --- | --- | --- | --- |
|  |  | Rev. No. | 00 |
|  | BROMINATED EPOXY OLIGOMER (CXB-714C) | Rev. Date | 2002. 07. 01 |
|  |  | PAGE | 1/1 |
| 1. APPLICATIONS |
| 1-1 CXB-714C is a brominated oligomeric flame retardant epoxy additive having a molecular weight of 1,250∼1,350. 1-2 It is recommended for use in ABS and HIPS. 1-3 Due to the oligomeric nature and chemical structure of CXB-714C it is non-blooming and exhibits high thermal stability, high UV stability and good processability. Having a relatively low softening range, it mixes and disperses readily into polymer system. |
| 2. CHEMICAL NAME & CHEMICAL STRUCTURE |
| Brominated Epoxy Oligomer |
| 3. PHYSICAL PROPERTIES |
| 3-1 Appearance : Pale Yellow Powder 3-2 Molecular Weight (GPC ) : 1,100 - 1,300 3-3 Softening Range : 100 - 110℃ 3-4 Bromine Content : 58 - 60% 3-5 Color (40%, Toluene) : 3 max.(Gardner) |
| 4. SOLUBILITY |
| 4-1 Insoluble : Water, Methanol 4-2 Soluble : DMF, Toluene, Acetone, Dioxane |
| 5. TOXICITY |
| LD50(oral, rat) : 2,000 mg/kg |
| 6. STORAGE & HANDLING |
| 6-1 CXB-714C is stable under normal condition. Store in cool and dry locations. 6-2 Avoid inhalation, ingestion and contact with skin and eyes. |

양식의 맨 위

# Text boxes

# WOOJIN

# COPOLYMER